TECHNICAL DATA SHEET

# KEROSENE LUBRICITY IMPROVER

DESCRIPTION:

Revol Kerosene Lubricity Improver is intended as an additive for kerosene being employed as a gas oil substitute in off-highway applications. Suitability of substituting Gas oil for kerosene should be assessed prior to use.

APPLICATIONS:

To be used in off highway applications only.

Typical treat @ 0.25% - 25Ltrs will treat 10,000ltrs of kerosene.

Typical application areas include off highway plant, agriculture and marine.

To be used in applications where there is concern over excessive wear from the use of kerosene.

Free from alcohol. Helps prevent corrosion and rust.

TYPICAL PHYSICAL CHARACTERISTICS:

Appearance                        Liquid

Density                               0.85 – 0.87 @ 15°C

Flash Point                         >180°C

Pour Point                          < - 10°C

Viscosity                            30.5 cSt @ 40°C

PACKAGING:

5 Ltr, 25 Ltr Drum, 205 Ltr Barrel, 1000 Ltr IBC.

CONTACT INFORMATION

Safechem Ltd. Drum House, Drum Industrial Estate, Birtley. Co. Durham DH21SR

Telephone: +44 (0) 191 410 8668

Email: sales@safechem.co.uk

Dated: May 2021